## Slide 1: Bonded Structures:- Certification Practices
Maxwell Davis PSM, B.Eng (Mech.), M. Eng (Mech.), PhD (honorary)
Director, Adhesion Associates Pty. Ltd.
www.adhesionassociates.com

## Slide 2: Prerequisite commentary
Current regulatory structure addresses strength, fatigue resistance, environmental protection, damage tolerance, materials and processes for adhesive bonded structures
Supported by Advisory Circulars and Policy Statement
There is one adhesive bond failure mode which is only indirectly addressed by the regulations and ACs.
An example of a crash probably related to this failure mode will be presented later in Adhesive Bond Failure Forensics
To understand this failure mode, some pre-requisite knowledge will be provided

## Slide 3: Processes and bond strength
Bonding processes affect short and long term bond strength
Short-term strength is dominated by production defects and in-process contamination
  Well designed and well processed bonds should last the life of the part
Long-term strength loss is totally dominated by the longevity of the bond interface
  Failure is NOT through the adhesive layer
  Determined by production surface preparation
Direct correlation between failure mode and bond strength

## Slide 4: Mechanism of adhesion
To understand interfacial longevity, understand how adhesives function
Adhesives depend upon chemical bonds formed at the interface between the adhesive and adherend
  Strong chemical bonds, failure occurs through the adhesive in the plane of the carrier cloth
    High bond strength
  Weak chemical bonds, failure occurs at the interface
    Low bond strength
Weak bonds may occur due to contamination during processes OR by degradation of the interfacial chemical bonds in service

## Slide 5: Mechanism of adhesion failure (metals)
Bonds to metals depend on maintaining chemical bonds at interface for the life of the part
Typically adhesives bond to surface oxides produced during surface preparation at the time of fabrication
Many metals are susceptible to hydration of surface oxides in later service e.g.
  Al2O3 Al2O3.2H2O
Chemical bonds between adhesive and metal dissociates- disbonding occurs at interface
Caused by moisture which diffuses through the adhesive
Disbonds may occur with no loads at all
Surface preparation must prevent hydration
Similar mechanism may occur in bonds to laminated composites?

## Slide 6: Adhesive bond failure types Metal and laminates
Four types of bond failure:
  Cohesion failure
    Adhesive layer is fractured
  Adhesion failure
    Separates from the surface of the adherend(s)
  Mixed-mode failure
    Variable combination of adhesion and cohesion failure
  Peel failure
    Cleavage of the joint by out-of-plane forces
COHESION FAILURE
ADHESION FAILURE
MIXED-MODE FAILURE
PEEL FAILURE

## Slide 7: Special failure mode for laminates
Laminated composites may exhibit a unique failure mode
Inter-laminar failure may peel the first ply off the laminate
  Peel stresses
  Shear stresses may exceed ILS
INTER-LAMINAR FAILURE

## Slide 8: Cohesion failure
Fails through carrier cloth
  Adhesive on both surfaces
Strength is high
Damage Tolerance is appropriate for managing macro-voids
  Design issues:
    Thermal stresses
    Stiffness mismatch (thickness, modulus)
    Inadequate bond overlap
    Inadequate service temperature range
    Peel stresses
  Production issue
    Bondline voids
  Operator issue
    Overload
Cohesion failure
NDI Effective
DTA Effective
Time
Strength
Required strength
Effective bond
Notes: 8

## Slide 9: Adhesion failure
Adhesion failure results when the interfacial chemical bonds fail
May result from:
  Contamination during processing
    Strength is always low
    Short service life before disbond occurs
  Inadequate adhesive cure
    Strength is always low
  Degradation of interfacial chemical bonds
    Strength is initially high but falls off with time
It is highly improbable that operator initiated actions can cause adhesion failures

## Slide 10: Between cohesion and adhesion?
Cohesion- strong
Adhesion- weak
Between, strength may be degraded
Failure will be mixed-mode blending into adhesion
Degradation rate depends on:
  Time
  Production process
  Edge distance
NDI detects bond separation
NDI can not detect strength loss until disbonding actually occurs
Effective bond
Time
Strength
Required strength
Cohesion failure
Adhesion failure
NDI Effective
Mixed -mode
NDI cannot detect strength loss
Notes: 10

## Slide 11: Explaining mixed-mode failures
Cohesion failure occurs through carrier cloth
As interface degrades:
  Failure locus moves towards interface
  Strength reduces
Eventually adhesion failure occurs at interface
  Very weak
Safety investigators note:
  A thin residue of adhesive on surfaces does NOT mean a strong bond
Notes: 11

## Slide 12: Let’s be clear
Regulations, DTA assume cohesion failure
Current NDI only finds disbonds after complete separation
  If structure has not already failed from low bond strength
  This may occur in the absence of any detectable disbond
DTA and NDI ineffective for adhesion, mixed-mode failures
  Also true for bond porosity
There is a real risk to continuing airworthiness by applying DTA to these defects
Effective bond
Cohesion
Mixed mode
Adhesion
NDI and DTA ineffective
Operating loads
Time
Strength
Required strength
Voids
Disbonds

## Slide 13: Now to the regulations……
Please read the full text of regulations and ACs
Applicable regulations are:
  2x.605 (Processes)
  2x.603 (Environmental effects)
  2x.573 (Damage tolerance)
2x.603: Must take into account environmental effects
  Almost all manufacturers address this by moisture conditioning
    Will NOT address interfacial degradation
2x.605: Processes must produce a “sound” structure
  Bonds which are susceptible to interfacial degradation initially appear “sound” yet strength decays with time
  2x.605 will not necessarily exclude processes which cause interfacial degradation

## Slide 14: Damage tolerance regulations
2x.573 paragraph 5: Limit load capability must be substantiated by one of the following methods:
  (i) The maximum disbonds of each bonded joint determined by analysis, tests, or both. Disbonds greater than this must be prevented by design features; or
  (ii) Proof testing must be conducted on each production article that will apply the critical limit design load to each critical bonded joint; or
  (iii) Repeatable and reliable non-destructive inspection techniques must be established that ensure the strength of each joint.
Each of these paragraphs will be discussed

## Slide 15: Disbond size determination
2x.573 5(i): maximum disbond determined by analysis or testing
  Traditionally involves:
    FEA modelled by disconnecting elements to represent disbond
    Testing using non-bonding inserts placed in bond
Effective for modelling production macro-voids
Does NOT represent:
  Bond porosity (multiple small voids, not one large disbond)
  Interfacial degradation because bond adjacent to defect is degraded
Test, analysis assume adhesive adjacent to defect is pristine
  In real structures interface adjacent to defect is degraded
    Discussed in Adhesive Bond Failure Forensics this afternoon

## Slide 16: Proof testing
2x.573 5(ii): Proof testing must be conducted on each production article that will apply the critical limit design load to each critical bonded joint
Because interfacial degradation is TIME dependent proof testing after production will NOT exclude possible weak bonds which occur in later service

## Slide 17: NDI for bond strength determination
2x.573 5(iii) requires NDI to determine bond strength (load capability)
Current NDI methods can not measure strength
  Potential for future developments
    Discussed in Adhesive Bonded Failure Forensics later
  Understand that even if NDI could measure post production strength this will STILL not prevent adhesion and mixed-mode failures
    Ongoing strength measurement will always be required to manage continuing airworthiness
  If production treatments prevent interfacial degradation it may be possible to reduce inspection frequency

## Slide 18: Guidance
Formal guidance is available from
  AC 20-107B Composite Aircraft Structure
  AC 23-19 Airframe Guide for Certification of Part 23 Airplanes
  AC 23-20 Acceptance Guidance on Material Procurement and Process Specifications for Polymer Matrix Composite Systems
AC 20-107B is the primary guidance document for adhesive bonded (composite) structures

## Slide 19: AC 20-107B para 6 Material and Fabrication Development
para c. Structural Bonding Sub para (1)
  Bond issues in service relate to invalid qualifications or insufficient QC
    Physical and chemical tests may be used (???)
  Lap shear tests common for adhesive, process qualification
    Shear tests do not provide a reliable measure of long-term durability and environmental degradation associated with poor bonding processes
    Peel testing has proven more reliable for evaluating proper adhesion
      Wedge testing advocated by PS-ACE100-2005-10038
  Without chemical bonding weak bonds may result from peel forces or environmental degradation, or both
  Adhesion failures are unacceptable failure mode in all test types
  Material or bond process problems that lead to adhesion failures are to be solved before proceeding with qualification tests
Note: No discussion of mixed-mode failure, the precursor to adhesion failure: Bonds may be weak before adhesion failure occurs

## Slide 20: Process validation
      Wedge test ASTM D3762 mentioned in PS-ACE100-2005-10038
ASTM D3762 (modified) recommended by TTCP Action Group 13 based on RAAF and USAF experience with on-aircraft bonded repair processes
  RAAF: 0.06% failures in 20 years- all due to technician malfunction: Solution? Full contact counselling
  USAF 0% failures in 15 years
FAA has program with Uni of Utah to redraft ASTM D3762
  How is it going Larry?
Should be adopted as minimum standard for bond longevity validation (equivalent or better…) in AC 20-107B

## Slide 21: AC 20-107B para 6 Material and Fabrication Development
Para c. Structural Bonding Sub para (2)
  Process specifications control essential for adhesive bonding in manufacturing and repair
  Combination of in-process inspections and tests have proven reliable
Comment: To prevent adhesion and mixed-mode bond failures it is essential that processes are validated to demonstrate bond longevity before certification testing starts and before the specifications are written

## Slide 22: AC 20-107B para 6 Material and Fabrication Development
Para c(2) environment
  The environment and cleanliness of facilities used for bonding processes are controlled to a level validated by qualification and proof of structure testing
  Adhesives and substrate materials are controlled to specification requirements that are consistent with material and bond process qualifications
  Bond surface preparation and subsequent handling closely controlled in time and exposure to environment and contamination
Comments are on the next slide

## Slide 23: Some important advice
Pay careful attention to interpretation of AC 20-107B para 6 c (2) advice about bonding environment
High humidity at the time of bonding can cause significant strength loss due to porosity
  FM300 adhesive 86F (29C), 70% RH, 4hrs exposure results in micro-voids
    53% loss of T-peel strength (ASTM 1876)
    28% loss of honeycomb peel strength (ASTM D1781)
NDI has difficulty finding porosity
This strength loss is NOT managed by FAR 2x.573 damage tolerance testing
Specifications must limit temperature and RH to the recorded certification production environment
Exceeding these limits is a safety risk

## Slide 24: AC 20-107B para 6 Material and Fabrication Development
Para c. Structural Bonding Sub para (2) refers to § 23.573(a)(5)
Limit load capacity must be substantiated by one of the following methods
  (i) The maximum disbonds of each bonded joint determined by analysis, tests, or both. Disbonds greater than this must be prevented by design features; or
  (ii) Proof testing must be conducted on each production article that will apply the critical limit design load to each critical bonded joint; or
  (iii) Repeatable and reliable non-destructive inspection techniques must be established that ensure the strength of each joint.
Repeated from 2x.573 as discussed previously

## Slide 25: AC 20-107B para 6 Material and Fabrication Development
Para c. Structural Bonding sub para (4)
  Adhesion failures in production require immediate action to identify the specific cause and isolate all affected parts and assemblies for disposition
  Adhesion failures in service require immediate action to determine the cause, to isolate the affected aircraft, and to conduct directed inspection and repair
    Depending on the suspected severity of the bonding problem, immediate action may be required to restore the affected aircraft to an airworthy condition
Comment: While this change addressed adhesion failures, the significance of mixed-mode failures is not addressed
  Mixed-mode failure can occur at loads significantly below limit load without adhesion failures being detectable prior to failure
I suggest that an appropriate amendment to AC20-107B is essential

## Slide 26: AC 20-107B para 6 Material and Fabrication Development
Para d Environmental Considerations
  The same environmental considerations in this section for composite materials also apply for adhesive bonds
    Effects of humidity and temperature in service must be considered
Notes:
    Temperature has a direct effect on adhesive properties
    Moisture reduces Glass Transition Temp. of adhesives and resins
      High temperature strength is lower
      Testing after moisture conditioning will address Tg effects
    Again, moisture conditioning will not address interfacial degradation

## Slide 27: Building block approach AC20-107B
Para 7a(3)b(1) Figure 1:
Extensive program to generate confidence in “design allowables”
  Most data is comparative, not actually used for design
Coupon tests
  Shear and peel strength
  Temperature, environment
  Multiple types of tests
Element tests
  Dissimilar materials
  Dissimilar thicknesses
Details
  ALL joint configurations tested
Sub-component and component tests demonstrate structural integrity
Data Base
Structural

## Slide 28: Average shear stress method
For adhesive bonds the Building Block approach is based primarily on designs using an average shear stress
Method used by 77% of US OEMs (FAA Workshop, Seattle 2004)
Calculate average shear stress
Compare against “design allowable”
  Determined from coupon tests
  Knock down factors allow for:
    Joint materials, thermal expansion, overlap length, adherend thicknesses, cure and service temperatures
The design allowable stress is set sufficiently low to assure bonds won’t fail for all design conditions and environments

## Slide 29: Average shear in adhesive bonds
The average shear stress design methodology is fundamentally flawed
Shear generated by displacement differences between members
If members were infinitely stiff, shear would be uniform
The average shear stress is calculated from
This suggests that if the overlap length was doubled, then the joint would carry twice the load- WRONG!
We don’t see failures due to design because of excessive knock-down factors used in design, and supporting testing

## Slide 30: Actual adhesive shear stresses
In REAL bonds, adherends strain non-uniformly
Peak shear stresses at joint ends, zero in middle
Load transfers only near ends of joint
Increasing overlap will NOT change shear stress
Strain Increasing
Strain Increasing
Shear
Stress

## Slide 31: One alternative to average shear
Possible to calculate bond load capacity
  The strength of the adhesive in the absence of adherend failure
    Based on analysis by Hart-Smith
Analysis actually calculates influence of:
  Adhesive properties
  Modulus of elasticity of adherends
  Thickness of adherends
  Coefficient of thermal expansion (CTE) of adherends and T between cure and operating temperatures
  Service temperature effects on adhesive properties
Higher level of confidence:- actual potential failure load is calculated
Average shear model manages these by knock down factors
If you want the equations email me max@adhesionassociates.com

## Slide 32: Applying the load capacity method
Analysis determines potential bond strength
Adherend strength linear with thickness
Adhesive strength depends on SQRT of adherend thickness
Left of cross-over, adherend is weaker than adhesive
  Adhesive will never fail
Right of cross-over adhesive is critical before structure
  Undesirable, must be supported by extensive testing
Overlap MUST be adequate
Processing must be valid
Shear
A
Bond stronger
B
Adherend at DUL
Adherend Thickness
Strength
Bond weaker
Notes: Hart-Smith, L.J., "Effects of Flaws and Porosity on Strength of Adhesive-Bonded Joints", Douglas Aircraft Company Report MDC J4699, November 1981.

## Slide 33: Design: Load capacity method
Design so adhesive is NOT critical at DUL
  Calculate potential strength of the adhesive
  Verify potential strength is above ultimate load + safety factor
  Adhesive will never fail at DUL
  Will readily meet limit load requirements
Analysis accounts for different joint parameters (E, t, CTE, ΔT
  Handled by design, not manipulating “allowables”
Processing and overlap must be acceptable
Adhesive will never be the locus of failure
Tests should always fail outside joint

## Slide 34: Building Block for load capacity
Coupon, element tests characterize adhesive design data
  Fewer tests required
Analysis actually addresses temperature, thicknesses, CTEs, moduli and adhesive properties
  Not knock down factors
  Higher confidence in joint designs
Detail and sub-component tests qualify joint design
  Demonstrate failure always occurs outside joint
Component tests validate design
If every tests fails in adherend, why do more tests?
Change of adhesive:
Measure adhesive properties and calculate to show equivalent load capacity
  Testing requirement is minimised
Full-scale test
Component
Number of tests decreasing 
Details Minimal
Sub-component Minimal
Coupon data Reduced
Elements Reduced

## Slide 35: AC 20-107B on repair
Para 10 (3) Repair.
  All bolted and bonded repair design and processing procedures .. shall be substantiated to meet the appropriate requirements.
  Safety concern with bond material compatibilities, bond surface preparation, cure thermal management, composite machining, special composite fasteners, and installation techniques, and the associated in-process control procedures.
In reality how is this being applied?

## Slide 36: Can someone tell me…
Bond surface preparation for repair: shall be substantiated to meet the appropriate requirements
There are recently certified aircraft with “scuff sand and solvent clean” as the approved process for metals in the approved SRM
This would never meet the requirements for the base design!!!!!
How was this approved?

## Slide 37: Can someone tell me ……
Safety concern with …cure thermal management
How can a repair be performed using ONE heater blanket and only one thermocouple with no regard to the substructure?
  One thermocouple cannot provide assurance of cure and prevention of overheat on even moderately complex structure
There are recently certified aircraft with this as the approved process for carbon composites with a 212ºF (100ºC) cure cycle without moisture removal from the composite
  Heating laminated composites above 212ºF (100ºC) carries a high risk of delamination due to absorbed moisture turning to steam
  Relying on ONE heater blanket and ONE thermocouple is a severe risk to either overheat damage or undercure of the adhesive
How was this approved?

## Slide 38: Adhesion failure due to poor heating
Adhesion failure may occur from poor temperature control
Adhesive may cross-link before wetting the surface
  Similar to time-expired adhesive
Sufficient contact to pass production NDI
Example: Single heater blanket repair to complex structure
Mixed-mode and cohesion
Adhesion
Notes: Adhesion failures can also occur if the adhesive fails to reach cure temperature during the cure cycle. Under these circumstances the adhesive may cross-link and gel before it has an opportunity to flow and wet the surface. A similar result would occur with the use of an adhesive that was “out of life”. Usually there may be sufficient contact to pass post-production NDI, but in-service failure may be inevitable.
In the example presented, a bonded repair was applied over thin skin attached to complex, thick sub-structure. The technician followed the approved SRM and used a single heater blanket. In the area where the skin was thin and there was sufficient heater blanket to locally achieve the cure temperature, the adhesive was correctly cured, as demonstrated by the cohesion failure of the bond when the repair was removed after the first in-service NDI inspection detected disbonding. However, over the thicker regions and over the thinner skin regions where the extent of overlap of the heater blanket was insufficient to achieve the cure temperature, there is clear evidence of adhesion failure.

## Slide 39: Can someone tell me…
To save time I’ll discuss injection “repairs” in the Adhesive Bond Failure Forensics talk later today….

## Slide 40: An observation on bonded repair resources
CACRC is addressing on-aircraft repair issues
One specific limitation is that the committee must follow OEM repair methodologies
If OEMs specify:
  Scuff sand and solvent clean preparation for metals
  Single heat sources irrespective of substructure
  Control and acceptance based on only one thermocouple
Then the CACRC outcomes will be of limited value
I suggest that there needs to be an AC which provides guidance to OEMs on minimum standards for on-aircraft repair processes

## Slide 41: Suggested amendments for AC 20-107B on repair
(3) Repair. All bolted and bonded repair design and processing procedures applied for a given structure shall be substantiated to meet the appropriate requirements. Of particular safety concern are the issues associated with bond material compatibilities, bond surface preparation (including drying, cleaning, and chemical activation to a standard which matches the requirements of the base design), cure thermal management including procedures for management of heat sinks and positioning of temperature sensors such that overheating of the structure is avoided and assurance of adequate cure of materials is achieved, and procedures for management moisture content of sandwich and laminated structures prior to heat application, composite machining, special composite fasteners, and installation techniques, and the associated in-process control procedures.

## Slide 42: Conclusions
The current FARs do not prevent (or at best may be interpreted in a manner that fails to address) the occurrence of adhesion and mixed mode failures in bonded joints
With very careful and guided interpretation of ACs and Policy Statements it may be possible* to develop reliable bonds ….but..
A better approach would be to amend AC 20-107B to specifically address adhesion and mixed mode failures
The requirements for bonded repair methodology needs to be significantly improved

## Slide 43: The crux of the problem
No effective feedback loop between adhesive bonding industry and regulators
  Adhesive strength can not be measured, and strength tests do not interrogate long term bond survivability
  Current regulatory and advisory framework does not adequately exclude adhesion and mixed-mode- failure, so process deficiencies are not redressed
  Short term there is no method to identify bad practices until failure occurs in later service but investigators and industry are not trained to identify bond failure modes and causes so deficiencies are not identified
  Industry is unaware of the causes of subsequent failures so mistakes are repeated because the processes are “approved” by strength testing
  There is a mentality of “blame the operator”……Buffing paint work causes interfacial bond failures???? Really?
  Failures are difficult to tie to the cause of a crash- are the bond failures the cause or the result? So production mistakes are not identified and corrected
A lot of industry does not even know that there is a bonding problem

## Slide 44
Question time
?
Notes: Intentionally blank

## Slide 45: Nomenclature
to
Elastic Modulus Eo
Coeff. of Thermal Expansion o
Subscripts
i = Inner adherend (structure)
o = Outer adherend (doubler)
1 = Outer end of joint
2 = Inner end of joint
Various standards for nomenclature
Variables used in this part of the course are:
Load P
Thermal Load T1
Thermal Load T2
ti
Elastic Modulus Ei
Coeff. of Thermal Expansion i

Shear Modulus G
Elastic strain e
Plastic strain p
Shear stress p
Load P1
Load P2

## Slide 46: Load capacity including thermal loads
The load capacity for dissimilar material, including thermal loads is derived from the lower value of:
The load capacity PLC is the lower value of
and
Notes: Hart-Smith, L.J., "Effects of Flaws and Porosity on Strength of Adhesive-Bonded Joints", Douglas Aircraft Company Report MDC J4699, November 1981.
Hart-Smith, L.J., Explanation of Delamination of Bonded Patches under Compressive Loads Using New Simple Bonded Joint Analyses, 6th Joint FAA/DoD/NASA Conference on Aging Aircraft, San Francisco, California, September 18-19, 2001.

## Slide 47: Adhesive design properties
Adhesive properties: Thick Adherend Test ASTM D5656
Shear stress vs shear strain
  Not just average shear stress
Test over entire service temperature range
Up to 80% of strain energy to failure from plastic behavior
Data adjusted to elastic-plastic model
  Conserves strain energy
True curve
Shear Stress
Shear Strain
G
Equal areas
Model
max
p
e
Notes: Hart-Smith, L.J. Adhesive Bonded Single Lap Joints, NASA CR 112236, Jan 1973

## Slide 48: Thick adherend test ASTM D5656
Thick adherends minimize strains in adherends
Shear strains measured by shear extensometer
Data modified to elastic-plastic model
This IS actual design data
Determine from tests
  Average shear stress at failure (p)
  Shear strain at elastic limit (e)
  Shear strain at failure (max) to derive plastic stain (p= max- e)
  Shear modulus (G)
Test over service temperature range
  Load capacity critical at low temperatures (-65F)
  High temperature case determines overlap length required
Exclude specimens with adhesion failure